## Slide 1: FATIGUE OF MATERIALS & STRUCTURES
G. Hénaff
1

## Slide 2: Fatigue of notched components

## Slide 3: Notch effect
r
s
x
2a
2h
⇒ The local stress at the notch root is higher than the gross stress

## Slide 4: Stress concentration factor
Definition : ratio “local stress/ gross stress on the net section”
Kt :
- is defined within the framework of elasticity;
- Only depends on geometry, in particular the notch tip radius! (typically not on the constitutive law of the considered material)
=

## Slide 5: Relation between Kt, Ks and Ke
K
s
s
y
Elastic domain
Elasto-plastic
Domain
K
e
>
K
t
>
K
s
K
t
=
K
s
=
K
e
K
e
K
t
,
K
e ,
K
s
s

## Slide 6: Reduction in fatigue life
Notch effect on fatigue limit quantified by the Kf cœfficient :
Sensitivity to notch effect :
q=0: insensitive to notch effect;
q=1 : no adaptation (Kf=Kt)

## Slide 7: Determination of the q coefficient
“Material” Parameter
Peterson: m=1
Neuber: m=1/2
Mild steels: a=0,25mm
High strength steels: a=0,025mm

## Slide 8: Determination of Kf or q

## Slide 9: Application to Wöhler curves
The determination of Kf permits the prediction of the fatigue life of notched components on the basis of the Wöhler curve established on smooth samples.

## Slide 10: Application to Wöhler curves
Data on smooth samples
Master curve

## Slide 11: Neuber’s Rule
Problem: determine the local stress/strain amplitude at the notch root from the far field loading
→ simple solution in the framework of elasticity:
Still valid in the easto-plastic domain
→ Idea: extrapolate the previous relation to the elasto-plastic domain

## Slide 12: Neuber’s Rule
Graphical solution of the equation:
s
e
The solution also behaves to the constitutive law of the material

## Slide 13: Extension to cyclic loading

## Slide 14: Equivalent Deformation Energy (EDE) criterion
Strain energy density in elasticity:
Hyp. : relation always satisfied in elasticity
s
e
Fictional elastic material
EDE : the two areas are equal
s
e

Neuber’s rule overestimates the local stress and strain
Actual material

## Slide 15: Comparison Neuber/EDE using Ramberg-Osgood constitutive law
EDE:
Neuber

## Slide 16: Application of Neuber’s rule : prediction of crack initiation in a suspension triangle
initiation